# Guardian Glass, LLC							        November 2020

2300 Harmon Road, Auburn Hills, Michigan 48326

Toll Free	(866) 482-7374

# Web Site	www.guardianglass.com

NOTICE: The guide specification on the following pages is designed to assist architects and specification writers. It is provided as a guideline only. Guardian Glass does not assume any responsibility for the suitability or applicability of this guide specification to any specific building project. Please activate “View Hidden Text” when using this guide specification to see specifier notes.

## Guide Specification in CSI 3-Part Format

Specifier Notes:  This guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, contained in the CSI Manual of Practice.

The section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the drawings.

Delete all “Specifier Notes” when editing this section.

## SECTION 088100

## BIRD-FRIENDLY DESIGN, LOW-E COATED, CLEAR INSULATING LAMINATED GLASS

- GENERAL

      - Summary

        - Section includes double-glazed bird-friendly low-E coated insulating glass units with laminated outboard lite.

        - Related Sections:

          - Division 02-49 Sections specifying glass and glazing by reference to this Section.

          - Division 07 Section "Joint Sealants" for glazing sealants.

          - Division 08 Section "Decorative Glass Glazing" for decorative glass for interior applications.

          - Division 08 Section "Mirrors" for interior, unframed glass mirrors.

          - Division 08 Section "Plastic Glazing" for acrylic and polycarbonate glazing.

          - Division 08 Section "Security Glazing" for security applications.

          - Division 10 Section "Toilet, Bath, and Laundry Accessories" for metal-framed mirrors.

      - REFERENCES

        - ASTM C 1036 - Standard Specification for Flat Glass.

        - ASTM C 1048 - Standard Specification for Heat-Treated Flat Glass--Kind HS, Kind FT Coated and Uncoated Glass.

        - ASTM C 1172 - Standard Specification for Laminated Architectural Flat Glass.

        - ASTM C 1376 - Standard Specification for Pyrolytic and Vacuum Deposition Coatings on Glass.

        - ASTM E 2188 - Standard Test Method for Insulating Glass Unit Performance.

        - ASTM E 2190 - Standard Specification for Insulating Glass Unit Performance and Evaluation.

        - CPSC 16CFR-1201 - Safety Standard for Architectural Glazing Materials.

        - ASTM E 1886 - Test Method for Performance of Exterior Windows, Curtain Walls, Doors and Storm Shutters Impacted by Missile(s) and Exposed to Cyclic Pressure Differentials.

        - ASTM E 1996 - Standard Specification for Performance of Exterior Windows, Curtain Walls, Doors and Storm Shutters Impacted by Windborne Debris in Hurricanes.

        - CPSC 16CFR-1201 - Safety Standard for Architectural Glazing Materials.

        - GANA Glazing Manual.

        - GANA Laminated Glazing Reference Manual

      - DEFINITIONS

        - Sealed Insulating Glass Unit with Laminated Outboard Lite Surfaces:

          - Surface No. 1:  Exterior surface of outer lite.

          - Surface No. 2:  Interior surface of outer lite.

          - Surface No. 3:  Exterior surface of inner lite.

          - Surface No. 4:  Interior surface of inner lite.

          - Surface No. 5:  Exterior Surface of inboard lite.

          - Surface No. 6:  Interior Surface of inboard lite.

        - Airspace:  Space between lites of an insulating glass unit that contains dehydrated air or other inert specified gas.

      - SUBMITTALS

        - Comply with Division 01 Section "Submittal Procedures."

        - Product Data:  Submit manufacturer's product data, including performance characteristics and installation instructions.

        - Shop Drawings:  Submit manufacturer's or fabricator's shop drawings, including plans, elevations, sections, and details, indicating glass dimensions, tolerances, types, thicknesses, and coatings.

        - Samples:  Submit manufacturer's samples of each type, thickness, and coating.

        - Fabricator's Certification:  Submit fabricator's certification by manufacturer.

        - Cleaning Instructions:  Submit manufacturer's cleaning instructions.

        - Warranty:  Submit manufacturer's standard warranty for sealed insulating glass units.

      - QUALITY ASSURANCE

        - Manufacturer's Qualifications:  Minimum of 5 years experience manufacturing solar control coated glass.

        - Fabricator's Qualifications:

          - Minimum of 5 years experience manufacturing sealed insulating glass units meeting ASTM E 2190.

          - Minimum of 5 years experience manufacturing Laminated glass units meeting ASTM C 1172 and CPSC 16CFR-1201.

          - Certified by manufacturer.

Retain first paragraph below if required by Project. The IBC defines wind-borne debris regions. Enhanced protection applies to essential facilities. Verify requirements of authorities having jurisdiction.

        - Windborne-Debris-Impact Resistance: Provide exterior glazing that passes [basic] [enhanced]-protection testing requirements in ASTM E 1996 for [Wind Zone 1] [Wind Zone 2] [Wind Zone 3] [Wind Zone 4] when tested according to ASTM E 1886. Test specimens shall be no smaller in width and length than glazing indicated for use on the Project and shall be installed in same manner as glazing indicated for use on the Project.

Retain first two subparagraphs below or retain third subparagraph–if required by Project. First two subparagraphs are requirements stated in the IBC; third is requirement in ASTM E 1996 for essential facilities.

          - Large-Missile Test: For glazing located within 30 feet of grade.

          - Small-Missile Test: For glazing located more than 30 feet above grade.

          - Large-Missile Test: For all glazing, regardless of height above grade.

        - Mock-Ups:

          - Comply with Division 01 Section "Quality Control."

          - Obtain acceptance of mock-ups by Architect before proceeding with work.

      - DELIVERY, STORAGE, AND HANDLING

        - Delivery:

          - Deliver glass to site in accordance with manufacturer's instructions.

          - Deliver glass in manufacturer's or fabricator's original containers and packaging, with labels clearly identifying product name and manufacturer.

        - Storage:

          - Store glass in accordance with manufacturer's instructions.

          - Store glass in clean, dry area indoors.

          - Protect from exposure to direct sunlight and freezing temperatures.

          - Apply temporary coverings loosely to allow adequate ventilation.

          - Protect from contact with corrosive chemicals.

          - Avoid placement of glass edge on concrete, metal, and other hard objects.

          - Rest glass on clean, cushioned pads at 1/4-points.

        - Handling:

          - Handle glass in accordance with manufacturer's instructions.

          - Protect glass from damage during handling and installation.

          - Do not slide 1 lite of glass against another.

          - Do not use sharp objects near unprotected glass.

      - WARRANTY

        - Manufacturer's Special Warranty on Laminated Glass: Manufacturer's standard form in which laminated-glass manufacturer agrees to replace laminated-glass units that deteriorate within specified warranty period. Deterioration of laminated glass is defined as defects developed from normal use that are not attributed to glass breakage or to maintaining and cleaning laminated glass contrary to manufacturer's written instructions. Defects include edge separation, delamination materially obstructing vision through glass, and blemishes exceeding those allowed by referenced laminated-glass standard.

Verify available warranties and warranty periods with manufacturers listed in Part 2 articles. Note that glass manufacturers typically begin the warranty period at the date of manufacture.

          - Warranty Period: [Five] [10] <Insert number> years from date of [manufacture].

- PRODUCTS

      - MANUFACTURER

        - Guardian Glass, LLC, 2300 Harmon Road, Auburn Hills, Michigan 48326.  Toll Free (866) 482-7374. Web Site www.guardianglass.com.

        - Substitutions:

          - Not permitted.

      - FABRICATORS

        - Sealed Insulating Glass Units, Laminated Glass Units, Heat-Strengthened Glass, Tempered Glass, and Spandrel Glass:

        - Acceptable Fabricators: Certified by glass manufacturer.

      - DOUBLE-GLAZED BIRD-FRIENDLY LOW-E COATED INSULATING GLASS UNITS WITH LAMINATED OUTBOARD LITE

Specifier Notes:  Guardian Bird1st™ UV Glass configurations are available on Guardian UltraClear® glass and clear glass substrates. Choose one of the two sections below to specify the desired substrate: 2.3.A for Guardian UltraClear® substrate or 2.3.B for clear substrate. Delete the unused section.

        - Double-Glazed Sputter-Coated Insulating Glass Units with UltraClear® Laminated Outboard Lite:

          - Conformance:  ASTM E 2190.

          - Conformance:  ASTM C 1172 and complying with testing requirements in CPSC 16CFR-1201 for Category II materials and with "Windborne-Debris-Impact Resistance" Paragraph in "Quality Assurance" Article.

          - Outboard Lite: Guardian UltraClear® Float Glass: ASTM C 1036, Type 1, Class 1, Quality q3.

            - Coating on Surface No. 1: Guardian Bird1st™ UV.

            - Coating Installation Orientation: Perpendicular (vertical) to the horizon.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

            - Interlayer:  Polyvinyl butyral (PVB) plastic interlayer, clear, 0.060 inch thick.

            - Inner Lite: Guardian UltraClear® Float Glass: ASTM C 1036, Type 1, Class 1, Quality q3.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [None] [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

          - Interspace thickness: 12.7 mm (1/2 inch) wide, hermetically sealed, dehydrated air space.

          - Interspace content: Air

          - Inboard Lite:

            - Guardian UltraClear® Float Glass:  ASTM C 1036, Type 1, Class 1, Quality q3.

            - Vacuum Deposition Sputtered Coating: ASTM C 1376.

            - Coating on No. 5 surface: SunGuard® Neutral 78/65.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [None] [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

          - Glass Unit Performance Characteristics:

            - Visible Light Transmittance:  80 percent.

            - Visible Light Reflectance Outdoors:  13 percent.

            - Direct Solar Energy Transmittance:  61 percent.

            - Direct Solar Energy Reflectance Outdoors:  18 percent.

            - Winter U-Value Nighttime:  0.30

            - Summer U-Value Daytime:  0.29

            - Shading Coefficient:  0.78

            - Solar Heat Gain Coefficient:  0.68

            - Summer Relative Heat Gain:  160

Retain one sealing system from options in first subparagraph below or insert other combinations; coordinate with manufacturers and products selected.

          - Sealing System: Dual seal, approved by glass manufacturer, with [polyisobutylene and polysulfide] [polyisobutylene and silicone] [polyisobutylene and hot-melt butyl] [polyisobutylene and polyurethane] primary and secondary.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

            - VOC Content: For sealants used inside of the weatherproofing system, not more than 250 g/L when calculated according to 40 CFR 59, Subpart D.

If retaining a specific spacer material, coordinate with manufacturers and products selected. Modify as required for "warm-edge" technology products

          - Spacer: [Manufacturer's standard spacer material and construction] [Aluminum with mill or clear anodic finish] [Aluminum with black, color anodic finish] [Aluminum with bronze, color anodic finish] [Aluminum with powdered metal paint finish in color selected by Architect] [Galvanized steel] [Stainless steel] [Polypropylene covered stainless steel in color selected by Architect] [Thermally broken aluminum] [Nonmetallic laminate] [Nonmetallic tube] <Insert material>.

Revise subparagraph below if a specific type of desiccant is required.

          - Desiccant: Molecular sieve or silica gel, or blend of both.

Revise subparagraph below if specific types of corner construction are required.

          - Corner Construction: [Manufacturer's standard] [Soldered, welded, or bent; keyed joints and corners are not permitted].

        - Double-Glazed Sputter-Coated Insulating Glass Units with Clear Laminated Outboard Lite:

          - Conformance:  ASTM E 2190.

          - Conformance:  ASTM C 1172 and complying with testing requirements in CPSC 16CFR-1201 for Category II materials [and with "Windborne-Debris-Impact Resistance" Paragraph in "Quality Assurance" Article.

          - Outboard Lite: Guardian Clear Float Glass: ASTM C 1036, Type 1, Class 1, Quality q3.

            - Coating on Surface No. 1: Guardian Bird1st™ UV.

            - Coating Installation Orientation: Perpendicular (vertical) to the horizon.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

            - Interlayer:  Polyvinyl butyral (PVB) plastic interlayer, clear, 0.060 inch thick.

            - Inner Lite: Guardian Clear Float Glass: ASTM C 1036, Type 1, Class 1, Quality q3.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [None] [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

          - Interspace thickness: 12.7 mm (1/2 inch) wide, hermetically sealed, dehydrated air space.

          - Interspace content: Air

          - Inboard Lite:

            - Guardian Clear Float Glass:  ASTM C 1036, Type 1, Class 1, Quality q3.

            - Vacuum Deposition Sputtered Coating: ASTM C 1376.

            - Coating on No. 5 surface: SunGuard® Neutral 78/65.

            - Glass Thickness: 6 mm (1/4 inch).

Specifier Notes:  Specify the method of heat treatment.  Guardian recommends substituting heat-strengthened float glass material for tempered fabrication, unless required by code or wind load.

            - Heat Treatment: [None] [Heat-strengthened, ASTM C 1048, Kind HS] [Tempered; ASTM C 1048, Kind FT; CPSC 16CFR-1201].

          - Glass Unit Performance Characteristics:

            - Visible Light Transmittance:  76 percent.

            - Visible Light Reflectance Outdoors:  12 percent.

            - Direct Solar Energy Transmittance:  48 percent.

            - Direct Solar Energy Reflectance Outdoors:  13 percent.

            - Winter U-Value Nighttime:  0.30

            - Summer U-Value Daytime:  0.29

            - Shading Coefficient:  0.67

            - Solar Heat Gain Coefficient:  0.58

            - Summer Relative Heat Gain: 137

Retain one sealing system from options in first subparagraph below or insert other combinations; coordinate with manufacturers and products selected.

          - Sealing System: Dual seal, approved by glass manufacturer, with [polyisobutylene and polysulfide] [polyisobutylene and silicone] [polyisobutylene and hot-melt butyl] [polyisobutylene and polyurethane] primary and secondary.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

            - VOC Content: For sealants used inside of the weatherproofing system, not more than 250 g/L when calculated according to 40 CFR 59, Subpart D.

If retaining a specific spacer material, coordinate with manufacturers and products selected. Modify as required for "warm-edge" technology products

          - Spacer: [Manufacturer's standard spacer material and construction] [Aluminum with mill or clear anodic finish] [Aluminum with black, color anodic finish] [Aluminum with bronze, color anodic finish] [Aluminum with powdered metal paint finish in color selected by Architect] [Galvanized steel] [Stainless steel] [Polypropylene covered stainless steel in color selected by Architect] [Thermally broken aluminum] [Nonmetallic laminate] [Nonmetallic tube] <Insert material>.

Revise subparagraph below if a specific type of desiccant is required.

          - Desiccant: Molecular sieve or silica gel, or blend of both.

Revise subparagraph below if specific types of corner construction are required.

          - Corner Construction: [Manufacturer's standard] [Soldered, welded, or bent; keyed joints and corners are not permitted].

      - FABRICATION OF GLAZING UNITS

        - Fabricate glazing units in sizes required to fit openings indicated for Project, with edge and face clearances, edge and surface conditions, and bite complying with written instructions of product manufacturer and referenced glazing publications, to comply with system performance requirements.

        - Fabricate laminated glass to produce glass free of foreign substances and air or glass pockets.

- EXECUTION

      - EXAMINATION

        - Examine areas to receive glass.  Notify Architect of conditions that would adversely affect installation.  Do not proceed with installation until unsatisfactory conditions are corrected.

      - PREPARATION

        - Verify glazing openings are correct size and within tolerance.

        - Verify glazing channels, recesses, and weeps are clean and free of obstructions.

      - GLAZING

        - Install glass in accordance with manufacturer's instructions, except where local codes or GANA Glazing Manual indicate more stringent requirements.

      - FIELD QUALITY CONTROL

        - Coated glass, when viewed from minimum of 10 feet, exhibiting slightly different hue or color not apparent in hand samples, will not be cause of rejection of glass units, as determined by Architect.

        - Verify glass is free of chips, cracks, and other inclusions that could inhibit structural or aesthetic integrity.

      - CLEANING

        - Clean glass promptly after installation in accordance with manufacturer's instructions.

        - Remove labels from glass surface.

        - Do not use harsh cleaning materials or methods that would damage glass.

      - PROTECTION

        - Protect installed glass from damage during construction.

        - Protect installed glass from contact with contaminating substances resulting from construction operations.

        - Remove and replace glass which is broken, chipped, cracked, abraded, or damaged in other ways during construction period, including natural causes, accidents, and vandalism.

## END OF SECTION